Fosroc Conbextra C

General purpose, flowable, dual shrinkage compensated, cementitious grout – 
(Gaps 10mm to 100mm thickness)

*1.0

Grouting Requirements

To the nominated area(s) (specify details and areas of application), grouting must be carried out using a pre-packaged, chloride and hydrogen gas free, dry powder blend of cements, graded fillers and chemical additives.

It is to be mixed with clean water to the required consistency. The plastic grout must not bleed or segregate. The storage, handling and placement of the grout must be in strict accordance with the manufacturer’s instructions.

A positive volumetric expansion of 1-3% shall occur while the grout is plastic by means of a gaseous system. Additionally the grout is to be formulated to compensate for longer term expansion in the hardened state.

It shall exhibit Flow Characteristics when tested to AS 1478.2.2005 of 400 – 600mm using the flow trough procedure.

It shall be formulated to exhibit the following characteristics when mixed with 3.6-3.9 lts water to one 20kg bag of the specified grout, at flowable consistency, when tested @ 23ºC:

Compressive Strength 	1 day 25MPa

(AS 1478.2.2005) 		7 days 45MPa

28 days 55MPa

Indirect Tensile Strength 	1 day 2.7Mpa

(AS 1012.11 – 2000) 		7 days 4.4MPa

28 days 4.8

Modulus of Rupture 		1 day 5.0MPa

(Flexural Strength) 		7 days 9.5MPa

(AS 1012.11 – 2000) 		28 days 9.6MPa

Fosroc Conbextra C manufactured by Parchem Construction Supplies meets the performance criteria and is approved for this application.