Proofex Engage

High performance, pre-applied membrane system, that mechanically bonds to poured concrete

1.0

Waterproofing

1.10

Basement concrete slab / wall protected membrane

1.11

The waterproofing membrane shall be a pre-applied membrane, that mechanically bonds to poured concrete, remaining in place if settlement occurs. The complex cell mesh bonded to a polyethylene membrane allows poured concrete to interlock with the membrane forming a strong mechanical bond. The membrane shall incorporate a peel-off selvedge strip to ensure sealed laps.

1.12

The membrane shall provide a long term protection to reinforced concrete in Australian climatic and environmental conditions and basement waterproofing protection to grades 2, 3, and 4, as specified in BS8102.

1.13

The membrane is to be installed completely in accordance with the current supplier technical data sheet.

All work shall be carried out by a pre-qualified contractor, who is well trained in the application of the specific, documented, membrane system.

1.14

All materials including membranes, used in conjunction with the new membrane system, shall be compatible with each other and be approved by the membrane supplier operating the ISO9001 or 9002 quality assurance scheme..

1.15

All materials are to be applied strictly in accordance with the supplier’s instructions and must be capable of being applied both horizontally and vertically using one grade of membrane, and laps between rolls must not encroach into the concrete cover.

1.16

The waterproofing membrane shall conform to the following performance properties:

| Minimum thickness | 4mm (0.8mm excl. Mesh) |  |
| --- | --- | --- |
| Elongation (peak) | 600% | ASTM D412 |
| Peel Adhesion to concrete | 74 N/50mm wide strip | BS 4254 |
| Shear strength of joints selvedge strip: | >377N at 50mm wide >506N at detail strip | MOAT 27:5.2.2 |
| Puncture resistance: | 600N | ASTM E 154 |
| Water vapour permeability: | 0.08gm-2 24hrs-1 | BS 3177 |
| Hydrostatic pressure resistance: (up to 70M head of water) | No leak after 1 hour | ASTM D5385 |

1.17

Fosroc Proofex Engage waterproofing membrane system from Parchem Construction Products meet the performance criteria and is an approved product for this application.